Schematic presentation of the proposed patterning approach

SEM imaging of a GC electrode modified with electrodeposited Au nano-particles. A) 5 second deposition, B) 15 seconds deposition.

SAM formation onto Au (b) and Au/Cu (c) electrodes compared with clean Au response (a): Cv of  1mM Ru(NH3)6+3  solution in 0.1 M PBS buffer

Effect of alkane thiol length on the stripping of Cu from an alkane thiol modified Au surface

Cyclic voltammogram (Scan rate 0.05 Vs-1) in 1 M NaClO4 of FcC6SH self assembled electrodes; a) Cu modified electrode with 1-undecanethiol SAM without Cu stripping, b) Au electrode with 1-undecanethiol SAM, c) Cu modified electrode with 1-undecanethiol SAM with Cu stripping.

Evaluation of a DQA0201 sensing platform prepared on the nano-patterned electrode. Control: full assay performed on a nano-patterned electrode without target hybridisation step. Target after Cu strip: full assay on a nano-patterned electrode. Target before Cu strip: full assay on an non patterned electrode. Backfilling bare Au: full assay on a genosensor prepared on a Au electrode according to the backifilling approach. Backfilling on modified Au: full assay on a genosensor prepared from a Cu modified Au electrode using the backfilling approach. Amperometric measurements performed in 10 mM tris buffer (pH 7.4) containing 500 mM NaCl. Enzyme (HRP) substrate (H2O2) and mediator (HQ) 2 mM

Calibration curves performed using the designed DF508 specific fluorescence MB for wild type and mutant sequences.

Example of the instability of the electrochemical response obtained for a Ferrocene modified E-MB.

Example of the stability of the electrochemical response obtained for a Methylene Blue modified E-MB.

Cross reactivity studies for the DF508 and V520F specific E-MB designed in the NanoSens project